## Slide 1: Introduction
The prime intent of fluid analysis is to evaluate the overall fluid condition for the purpose of:
  Monitoring fluid change intervals
  Monitoring fluid contaminates
    Glycol
    Water
    Silicon based particles
  Monitoring wear metals
Lab tests alone cannot consistently predict impending transmission failure
Wear metal test results can be indicative of internal wear
  Results must be analyzed carefully
  Use in conjunction with other inspection procedures
    Oil pan/filter contents

## Slide 2: Allison Approved Fluids
Vital to transmission reliability and durability
Transmission fluid functions
  Hydrodynamic energy medium for use in torque converter
  Hydrostatic energy medium for use in hydraulic control circuits
  Lubricating medium
  Sliding friction energy medium for clutches
  Heat transfer medium
  Act as sealant to help improve the ability of seals with maintaining hydraulic pressure

## Slide 3: Allison Approved Fluids
Transmission fluid functions (cont’d)
  Operate over a wide temperature range
    Provide stability and essential lubricating flow at low temperature
    Maintain lubricating qualities and fluid film thickness at elevated temperatures
  Compatibility with a variety of seal materials
  Maintain contaminate suspension introduced in, or generated by, transmission
  Provide a level of oxidation resistance
  Minimize fluid foaming
    Reduces fluid film and clutch apply force

## Slide 4: Allison Approved Fluids
Transmission fluid functions (cont’d)
  Remain non-corrosive to all transmission components
  Create protective barrier between operating surfaces
    Prevents/minimizes component contact

## Slide 5: Operating Environment
Effects fluid life
Applies to both natural and synthetic fluids
Transmission fluid reacts to its environment and the demands placed on it
Factors that directly effect fluid life
  Amount of oxygen in fluid (oxidation)
  Fluid temperature
  Wear particles
  Transmission duty cycle

## Slide 6: Oxidation
Most deciding factor in limiting functional life of transmission fluid
Chemical reaction between transmission fluid and oxygen
Catalytic effect takes place once reaction begins
  Results in formation of acids and iron oxide
Introduction of these byproducts reduce overall fluid performance

## Slide 7: Oxidation
Oxidation speed depends on environmental conditions
  Amount of oxygen subjected to fluid
    Air flow through transmission breather
    Fluid aeration related to incorrect fluid level
  Fluid temperature
    Oxidation rate doubles for every 10C/18F degree increase in fluid temperature
  Transmission operational time
  Presence of catalysts
    Water
    Copper
    Aluminum
    Contaminants

## Slide 8: Interpreting Fluid Analysis Results
Viscosity
  First property to experience measurable change during operation
  Affected by oxidation and shear
  Shear is a normal occurrence in fluids containing Viscosity Index (VI) improvers
  VI improvers are polymer chains
    Temperature sensitive
    Tightly coiled at low temperature
      Have little or no effect on viscosity
    Fluid temperature increase causes polymer chains to unwind
      React with one another to cause viscosity increase in fluid
    Improve fluid viscosity levels of fluid at elevated temperatures

## Slide 9: Interpreting Fluid Analysis Results
Viscosity (cont’d)
  Shear
    Function of time and operational severity
    Occurs when polymer passes through a low clearance, high stress meshing interface
      Planetery gears
      Charging pump
      Clutch plates
      Retarder
      Torque converter
    Polymer chains are cut or “sheared” into smaller pieces
      Begins to reduce elevated temperature viscosity of fluid
        Happens almost immediately
        Continues at a decreasing rate over life of fluid until base stock viscosity is reached

## Slide 10: Interpreting Fluid Analysis Results
Viscosity (cont’d)
  Viscosity is measured in centistokes (cSt) at 40C and 100C temperatures
  New, unused TES 295/TES 389 fluid
    Viscosity of 7.5 cSt at 100C
    Maximum viscosity change is +/- 25%
  Viscosity change example
    New TES 389 fluid with 7.5 cSt viscosity at 100C
      After operational time same fluid has viscosity of 5.2 cSt at 100C
    Fluid has experience a 31% change in viscosity

## Slide 11: Interpreting Fluid Analysis Results
Acidity
  Total Acid Number (TAN) is measure of fluid acidity
  Advanced oxidation always accompanied by presence of acid
    Measured by adding potassium hydroxide (KOH) to fluid sample until color changes
    Acidity is expresses as milligrams of KOH required to neutralize a gram of fluid
  Maximum allowed TAN change is +3.0%
    Measured against level of a new fluid

## Slide 12: Interpreting Fluid Analysis Results
Acidity (cont’d)
  Surface contact between mating components increases as fluid viscosity decreases
    Creates friction and wear between components
      Wear amount depends on load at mating surfaces
  Oxidation Example
    High load area of 3000/4000 charging pump busing and stator shaft journal mating surface
      Constant hydraulic pressure generation at this location creates high radial loads

## Slide 13: Interpreting Fluid Analysis Results
Acidity (cont’d)
  Oxidation Example (cont’d)
    High load area of 3000/4000 charging pump busing and stator shaft journal mating surface
      Constant hydraulic pressure generation at this location creates high radial loads
      Continues friction causes bushing to move in charging pump drive gear
      Radial movement progresses to both radial and axial movement
      Axial movement imposes load on side of charging pump drive tangs
        Tangs will eventually fracture
    Wear found on this journal indicates fluid is oxidized beyond Allison maximum oxidation limits
      Can also indicate use of non-Allison approved fluid

## Slide 14: Interpreting Fluid Analysis Results
Glycol and Water
  Most common and harmful contaminants found in transmission fluid
  Water
    Poor lubricant
    Promotes rust
    Leads to component failure
    Affects clutch plates
      Penetrates facing of friction clutch plate and rusts steel core
        Causes separation of friction material from core
      Presence of water in friction material greatly reduces fluid frictional resistance during clutch apply
        Excessive friction converts water to steam, damaging plate’s frictional material

## Slide 15: Interpreting Fluid Analysis Results
Glycol and Water (cont’d)
  Glycol
    Elements found in glycol attack bonding agents binding clutch plate friction material together and to the steel core
      Results in de-bonding of friction material from core
    Identified on analysis report as negative or positive
      No trace (positive reading) is allowed
      Not always identified by lab due to evaporation or lab error
    Presence can be visually identified in fluid
      Causes fluid discoloration
        Lighter in color (pink/orange)
      Applies to water contamination as well

## Slide 16: Interpreting Fluid Analysis Results
Glycol and Water (cont’d)
  Presence of rust is key indicator of water/glycol contamination
    Look specifically for presence of Sodium (Na) and Potassium (K) in lab report
      Presence greater than 10 parts per million (ppm) indicates glycol contamination even if report shows negative for glycol
        Elements almost always found singularly or together in glycol
      Presence of high Na without K can indicate presence of road salts in transmission
        Inspect dipstick fill tube seals for deterioration or improper alignment
        Inspect breather area for accumulation of road salts
        Look for holes in transmission housing created by salt corrosion

## Slide 17: Interpreting Fluid Analysis Results
Glycol and Water (cont’d)
  Possible reasons for negative glycol report even though transmission exhibits contamination characteristics
    Fluid recently changed due to cooler failure/replacement
      Transmission operated sufficient amount of time to evaporate glycol/water form fluid
    Non-representative fluid sample provided to lab
    Excessive amount of time between sample collection and lab analysis

## Slide 18: Interpreting Fluid Analysis Results
Glycol and Water (cont’d)
  Any time glycol or water is present in a transmission
    Transmission must be completely disassembled and cleaned
    Replace parts per SIL 18-TR-98
    Draining and refilling transmission with new fluid is not an acceptable fix
      Will eventually lead to transmission failure
  Maximum limit for water is 0.2%
    Equal to 2000 ppm
    Calculated as follows
      2000 liters x total transmission fluid volume / 1,000,000 liters = liters of water
    Example calculation with total fluid volume of 30 liters
      2000 x 30 / 1,000,000 = 0.06 liters of water (60 ml)

## Slide 19: Interpreting Fluid Analysis Results
Visual example of 60 ml water compared to 19 liter container – 60 ml is 2nd black line on fluid sample bottle
Glycol/water contaminated Transmission fluid

## Slide 20: Interpreting Fluid Analysis Results
Wear metals
  Transmission components experience wear during normal operation
  Microscopic particles enter fluid
    Due to particles being smaller than micron rating of transmission filters
  Wear metal analysis monitors identity and levels of wear metals in fluid
    Documenting concentration levels of these particles over time provides information on wear rate of internal components
      Information is only meaningful when used in conjunction with a prescribed procedure

## Slide 21: Interpreting Fluid Analysis Results
Wear metals (cont’d)
  Absolute maximum wear metal values cannot be applied to a transmission due to many variables
    Transmission series
    Transmission applications
    Laboratory variance
    Laboratory interpretations
  Rendering universal limits is nearly impossible even within the same transmission series

## Slide 22: Interpreting Fluid Analysis Results
Wear metals (cont’d)
  Must be evaluated using a “trend line” approach
    Concentration of each wear metal from each transmission must be plotted over a period of time
      Line of “best fit” drawn through plotted points is considered the “trend line”
      Minimum of four data points must be present before trend line can be established
      First data point should be from new, unused sample of fluid
        Establishes baseline
    Concern and further evaluation should only occur when significant deviation from projected trend line is present
      Laboratory results alone cannot consistently predict impending transmission failure

## Slide 23: Interpreting Fluid Analysis Results
Wear metals (cont’d)
  Wear metal test results can be indicative of internal wear
    Results must be analyzed carefully
    Results must be used in conjunction with other inspection procedures
      Oil pan content inspection
  Identifying impending failure through monitoring involves a little luck
    Time between beginning and ultimate component failure is short
      Does not typically take months for complete failure
      Possible that last fluid sample has no significant deviations for wear metals
        Complete failure may occur before next fluid analysis

## Slide 24: Interpreting Fluid Analysis Results
Wear metals (cont’d)
  SIL 17-TR-96 provides recommended fluid sample intervals
    Very general recommendations
    Sample frequency based on:
      Transmission series
      Transmission operational time
      Transmission application
      Severity of service
  Example
    Expense to predict failure of a 2000 series in a school bus vs. 9800 series in an oil field application is vastly different
      Financial benefit of repairing transmission before failure is much greater with the 9800 series

## Slide 25: Interpreting Fluid Analysis Results
Wear metals (cont’d)
  Wear metal chart examples
    Shows wear metal values over a period of time
    Values can be/are influenced by:
      Transmission model
      Transmission vocation
      Transmission fluid type
    Values provided are from two 3000 series transmissions
      Operating in refuse vocation
      Using TranSynd fluid
      Both transmissions are in separate operating fleets

## Slide 26: Interpreting Fluid Analysis Results
Wear Metal Chart #1

## Slide 27: Interpreting Fluid Analysis Results
Wear Metal Chart #2

## Slide 28: Filters
Micron ratings of Allison filters and Allison required filtration levels are based on transmission design and developmental testing
Using non-genuine filters can result in:
  Degraded performance
  Increased wear
  Damage
  Additional lifecycle cost

## Slide 29: Filters
Capacitization
  Using filters with micron ratings less than Allison genuine or factory approved filters will require more frequent changes due to filter become full at a faster rate
    Filter changes are based on filter capacity and ability to flow an adequate amount of fluid
      Prevents operational problems
      Prevents component damage
  3000/4000 series transmissions utilize a non-bypass filtration system
    Some models do not provide a feature to alert operator of a capacitized filter requiring a change
      System does not monitor pressure difference between filter intake and outlet

## Slide 30: Filters
Capacitization (cont’d)
  Continual operating of a capacitized filter in a non-bypass system will:
    Reach a pressure differential sufficient to collapse filter
    Trapped filter debris is pulled into hydraulic system causing potential damage to:
      Charging pump
      Bushings
      Bearings
      Bearing/bushing surfaces
      Clutches
        Due to debris causing valves to stick in valve bores

## Slide 31: Filters
Filter change intervals are based on the use of Allison approved filters
Beginning in build year 2008
  2010, 3000 and 4000 series transmissions equipped with Filter Life Monitor
    Alerts operator when main and lube filters must be changed
    Vehicle manufacturer chooses whether or not this feature is installed in a vehicle

## Slide 32: Filters
Warranty considerations
  A transmission that experiences a failure that is equipped with a non-genuine filter does not immediately void warranty
    Allison Transmission cannot, by law, make warranty contingent upon using Allison approved filters
    BUT, warranty can be denied if failure is due to the non-approved filter
  Example
    Main and lube filters installed by the factory are printed with “Factory Installed” on filter top cap along with date of filter manufacture
      Aids in instances where transmission failure occurs and questions of filter type and maintenance arise

## Slide 33: Filters
Warranty considerations
  Example (cont’d)
    Image shows a prior design Gold Series filter with original date stamp
    Filter removed from transmission that failed due to an overheated clutch
      Transmission build date was July 2002
      Transmission failure occurred in 2007
      Could lead to conclusion that filter was from original factory installation
    Use caution when referencing date code on filter
      Service facilities typically buy filter kits in bulk
      Filter with date code of July 2008 could be installed during a fluid change in July of 2009

## Slide 34: Filters
Warranty considerations
  Example (cont’d)
    In instances where an Allison service facility does not perform many fluid/filter changes:
      Turn over of filter kits is slow
      Must determine from customer when last filter changes was completed and by whom

## Slide 35: Incorrect Fluid Level
High fluid level
  If fluid level is filled to a point where it is allows to contact rotating components, the fluid will become aerated
  Aerated fluid commonly causes:
    Erratic shifts
    Shift flare and/or slipping shifts
    Fluid discharge through transmission breather
    Elevated operating temperature
    Accelerated fluid oxidation
    Reduction in fluid lubricating film
    Possible vehicle performance issues
      When operating in coverter mode
    Reduced transmission retarder performance

## Slide 36: Incorrect Fluid Level
Low fluid level
  Can cause same issues as high fluid levels
  Fluid typically does not contain air bubbles
    Unless fluid is not in 100% contact with suction filter
  If fluid level become low enough:
    Ability of transmission to maintain adequate supply of lubrication is impacted

## Slide 37: Case Study – Low Fluid Level
Issue
  Customer complaining of shift flares when loaded
    Vehicle mileage at failure 334,111 (537,700 Km)
Transmission
  4560P (6610125477)
  Original with no previous transmission repairs
Vocation
  Dump truck

## Slide 38: Case Study #1
Steps taken
  Fluid level verified two gallons low by OEM dipstick
  Transmission fluid leak fount at PTO hydraulic fitting
  Fluid level corrected
  Transmission stall test performed
    Turbine speed did not remain stationary in 1st, 4th, 5th and 6th ranges
  Main pressure measured
    Results below specification
  Transmission control module removed
    Suction filter full of clutch material

## Slide 39: Case Study #1
Steps taken (cont’d)
  Transmission removed and disassembled which revealed:
    Overheat condition present only in P2 planetary gear set
    Metal discoloration dispersed evenly across gear set
      Indicates excessive temperature did not begin in localized area
Rear face of P2 carrier

## Slide 40: Case Study #1
Steps taken (cont’d)
  P2 spindle carriers cut into spindle retainer equally
    Caused by excessive friction between
      Carrier gears
      Bearings
      Spindles
    Excessive friction creates excessive heat
    High temperatures created in P2 planetary due to this friction
Front face of P2 carrier
P2 carrier bearings, spindles and gears not fused together

## Slide 41: Case Study #1
All friction plates show signs of excessive temperature
  C5 clutch pack severely burnt
    Lost most of its friction material

## Slide 42: Case Study #1
How could this condition be caused by low fluid level?
  Transmission most likely operated for extended periods in 5th and 6th ranges
    Due to only P2 showing excessive temperature effects
  5th and 6th ranges are overdrive in 3000/4000 series
    Rotational speed of main shaft is greatest in these ranges
    Power from engine is input into P2 planetary gear set by P2 carrier
      Connected to C2 clutch drive hub
      Driven by C2 clutch
  Low fluid level caused insufficient lubrication to C5 clutch pack
    Resulting in overheat of clutch friction material

## Slide 43: Case Study #1
How could this condition be caused by low fluid level? (cont’d)
  Condition worsened as rotation speed of output shaft increased
    Increased speed requires sufficient quantity of lubricating fluid to maintain “film” between clutch plates
  Friction material from C5 and C2 clutch plates collected by suction filter
    Ultimately restricting fluid flow through filter
  With C2 clutch pack applied in 5th and 6th ranges, clutch is severely overheated
    Due to excessive slip
      Occurred due to suction filter restriction

## Slide 44: Case Study #1
Restricted suction filter caused reduced main pressure
  Consequently caused reduced clutch pressures
Reduction in C2 clutch pressure caused clutch to slip and overheat

## Slide 45: Verifying Transmission Fluid Level
Always use the Oil Level Sensor
  If available and equipped on transmission
Next best method is Allison dipstick or sight gauge
If OEM dipstick is only available and any of Case Study #1 issues are present:
  DO NOT ASSUME THE DIPSTICK IS CORRECT
Refer to SIL 32-TR-93 for dipstick calibration procedure
  Verifies OEM dipstick is providing correct readings